OX

Buckleys H5 UCP1B PROXIMITY PROBE

Specifications are subject to change without notice.                                              ©2016 Aqua-Air Industries, Inc. – All rights reserved.

# Text boxes

639 Manhattan Blvd.

Harvey, LA 70058 USA

TEL:  (504) 362-8124

FAX:  (504) 362-3600

www.aquaairind.com

EMAIL sales@aquaairind.com

The UCP1B proximity probe is a lightweight and versatile instrument specifically designed to carry out underwater cathodic protection potential measurements.

The probe has been developed for use with manned or Remotely Operated Vehicles (ROVs) and comes complete with 3 metres of cable. Each probe is supplied with a Certificate of Inspection and Conformity.

By placing the UCP1B in close proximity to the surface under test, a voltage reading can be obtained on a suitable high impedance or digital voltmeter. The meter should be connected between the probe and a separate structure negative return.

The UCP1B is extensively used in a wide range of

applications including production and drilling platforms, ships’ hulls, jetties and other marine works.

FEATURES

- Hard wearing DELRIN body

- Half Cell can be replaced

- Lightweight design / Easy to use

- Suitable for fitting to manipulator arm

UCP1B product code: H5

TECHNICAL SPECIFICATION

Half Cell

Type: Silver/Silver Chloride screw-in

Output: ≈ +250mV VS SHE

Temperature coeff: -0.6mV per °C

Temperature range: 0 - 30 °C

Working life: 1 to 2

Unit

Designed for use with remote voltmeter

Minimum load impedance >10M Ohms

Weight: 0.5Kg

Size: 126mm long x 39mm diameter

Underwater cable: 3m long x 9mm

Depth of operation: 700m+

Packed weight (complete): 0.8Kg

Dimensions (packed): 26cm x 14cm x 30cm

* AAI is the Exclusive Distributor for Buckley's Subsea Products in the U.S.A. *